Supporting Information

The Competition Between Mechanical Stability and Charge Carrier Mobility in MA-based Hybrid Perovskites: Insight from DFT

Jung-Hoon Lee*,†,⊥, Zeyu Deng†, Nicholas C. Bristowe‡,§,

Paul D. Bristowe*,†, and Anthony K. Cheetham*,†

†Department of Materials Science and Metallurgy, University of Cambridge,

Cambridge CB3 0FS, UK

‡School of Physical Sciences, University of Kent, Canterbury

CT2 7NH, UK

§Department of Materials, Imperial College London, London SW7 2AZ, UK

*E-mail: jhlee.david@gmail.com, pdb1000@cam.ac.uk, ack30@cam.ac.uk

⊥Current address: Department of Physics, University of California, Berkeley CA 94720 USA

J-HL and ZD contributed equally

1. van der Waals functionals

Table S1 | Computed lattice parameters and the polycrystalline (orientationally-averaged) Young’s moduli E of the orthorhombic (o-)MAPbI3 structure using different exchange-correlation functionals compared to experiment.

| Functionals | Lattice parameters |  |  | E (GPa) |
| --- | --- | --- | --- | --- |
|  | a (Å) | b (Å) | c (Å) |  |
| PBEsol1 | 8.9762 | 12.6134 | 8.4362 | 20.087 |
| optB86b+vdW2,3 | 8.8576 | 12.6751 | 8.5610 | 20.526 |
| vdW-DF24 | 9.2098 | 13.1736 | 8.8246 | 18.201 |
| TS5 | 8.9843 | 12.7192 | 8.4960 | 22.677 |
| SCAN6 | 8.9474 | 12.7222 | 8.6123 |  |
| Exp.7 | 8.8657 | 12.6293 | 8.5769 | - |

2. Ionic radii

Table S2 | A comparison of computed effective radii of all ions obtained from our DFT calculations with those obtained from Shannon’s work.8

| A-site | Radius (Å) |  | B-site | Radius (Å) |  | X-site | Radius (Å) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | This work | Shannon’s radii |  | This work | Shannon’s radii |  | This work | Shannon’s radii |
| K+ | 1.31 | 1.55 | Sn2+ | 1.39 | - | Cl- | 2.04 | 1.78 |
| Rb+ | 1.51 | 1.63 | Pb2+ | 1.41 | 1.19 | Br- | 2.22 | 1.96 |
| Cs+ | 1.76 | 1.78 |  |  |  | I- | 2.47 | 2.20 |
| Fr+ | 1.87 | 1.80 |  |  |  |  |  |  |
| MA+ | 2.07 |  |  |  |  |  |  |  |

3. Hydrogen bonding-induced octahedral tilting

Figure S1 | Computed average bond angles (θw) as a function of the tolerance factor for (a) o-APbI3, (b) o-APbBr3, (c) o-APbCl3, (d) o-ASnI3, (e) o-ASnBr3, and (f) o-ASnCl3. Blue circles and orange squares show the inorganic and hybrid series respectively. Variations from the inorganic trend lines are denoted by black arrows with their magnitudes.

4. Enhancement of hydrogen bonding across the halogen series

Figure S2 | Computed average hydrogen-bonding index (H-index) for the three H atoms attached to N on a MA cation for the o-MABX3 hybrid series. Inset represents a schematic view of the three H stretching modes.

Figure S3 | Non-covalent interaction density isosurfaces for (a) o-MAPbI3, (b) o-MAPbBr3, (c) o-MAPbCl3, (d) o-MASnI3, (e) o-MASnBr3, and (f) o-MASnCl3. The isosurfaces were generated for s = 0.5 and -0.04 < ρ < -0.02 (ρ is the electron density and s is the reduced density gradient).

5. 3x3 matrix forms of the six different strain types

,		,

,	,

6. Directional dependence of the Young’s modulus E of o-MAPbI3 and o-CsPbI3

Figure S4 | Directionally-dependent Young’s modulus E of o-MAPbI3 (blue) and o-CsPbI3 (red) in the ba-, ac-, and bc-planes of the orthorhombic structure. Circles indicate the magnitude of E (GPa).

7. Polycrystalline elastic moduli

Table S3 | Computed lattice parameters, tolerance factor (TF) the polycrystalline Young’s modulus E, bulk modulus B, shear modulus G, and Poisson’s ratio ν of all halide perovskites. The Pnma space group was imposed during optimization of the lattice parameters.

|  | a (Å) | b (Å) | c (Å) | TF | E (GPa) | B (GPa) | G (GPa) | ν |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| KPbI3 | 8.961 | 11.887 | 7.911 | 0.69 | 18.455 | 15.699 | 7.076 | 0.304 |
| RbPbI3 | 9.074 | 12.116 | 8.001 | 0.73 | 16.964 | 15.107 | 6.461 | 0.313 |
| CsPbI3 | 9.142 | 12.489 | 8.119 | 0.77 | 18.427 | 15.977 | 7.045 | 0.308 |
| FrPbI3 | 9.092 | 12.608 | 8.302 | 0.79 | 17.342 | 16.109 | 6.566 | 0.321 |
| MAPbI3 | 8.858 | 12.675 | 8.561 | 0.83 | 20.526 | 18.999 | 7.775 | 0.317 |
| KPbBr3 | 8.379 | 11.139 | 7.552 | 0.69 | 19.818 | 18.143 | 7.519 | 0.318 |
| RbPbBr3 | 8.481 | 11.449 | 7.622 | 0.73 | 19.621 | 17.980 | 7.443 | 0.318 |
| CsPbBr3 | 8.483 | 11.770 | 7.872 | 0.78 | 20.658 | 19.894 | 7.784 | 0.327 |
| FrPbBr3 | 8.450 | 11.882 | 8.000 | 0.80 | 20.028 | 20.669 | 7.482 | 0.339 |
| MAPbBr3 | 8.543 | 11.959 | 7.971 | 0.84 | 24.798 | 22.853 | 9.399 | 0.319 |
| KPbCl3 | 7.986 | 10.674 | 7.234 | 0.69 | 21.977 | 21.144 | 8.282 | 0.327 |
| RbPbCl3 | 8.078 | 10.943 | 7.387 | 0.73 | 21.296 | 21.592 | 7.972 | 0.336 |
| CsPbCl3 | 8.077 | 11.282 | 7.613 | 0.78 | 21.876 | 23.184 | 8.146 | 0.343 |
| FrPbCl3 | 7.975 | 11.346 | 7.849 | 0.80 | 22.807 | 24.609 | 8.475 | 0.346 |
| MAPbCl3 | 8.252 | 11.442 | 7.588 | 0.84 | 26.119 | 25.575 | 9.821 | 0.330 |
| KSnI3 | 8.851 | 11.828 | 7.876 | 0.69 | 19.022 | 15.916 | 7.312 | 0.301 |
| RbSnI3 | 8.912 | 12.058 | 8.030 | 0.73 | 18.915 | 16.409 | 7.231 | 0.308 |
| CsSnI3 | 8.856 | 12.350 | 8.359 | 0.77 | 19.287 | 17.139 | 7.348 | 0.312 |
| FrSnI3 | 8.753 | 12.417 | 8.591 | 0.80 | 18.704 | 17.632 | 7.068 | 0.323 |
| MASnI3 | 8.797 | 12.495 | 8.499 | 0.83 | 23.271 | 19.104 | 8.971 | 0.297 |
| KSnBr3 | 8.292 | 11.073 | 7.469 | 0.69 | 20.645 | 19.176 | 7.817 | 0.321 |
| RbSnBr3 | 8.345 | 11.348 | 7.623 | 0.73 | 20.473 | 19.625 | 7.719 | 0.326 |
| CsSnBr3 | 8.289 | 11.629 | 7.928 | 0.78 | 20.920 | 20.801 | 7.851 | 0.332 |
| FrSnBr3 | 8.182 | 11.650 | 8.178 | 0.80 | 24.978 | 22.486 | 9.498 | 0.315 |
| MASnBr3 | 8.492 | 11.753 | 7.895 | 0.84 | 25.818 | 23.387 | 9.809 | 0.316 |
| KSnCl3 | 7.899 | 10.574 | 7.172 | 0.69 | 23.939 | 23.016 | 9.022 | 0.327 |
| RbSnCl3 | 7.950 | 10.856 | 7.333 | 0.73 | 22.353 | 23.020 | 8.352 | 0.338 |
| CsSnCl3 | 7.837 | 11.119 | 7.701 | 0.78 | 24.519 | 25.448 | 9.153 | 0.339 |
| FrSnCl3 | 7.824 | 11.131 | 7.860 | 0.81 | 29.611 | 26.096 | 11.294 | 0.311 |
| MASnCl3 | 8.281 | 11.232 | 7.481 | 0.85 | 30.836 | 27.927 | 11.716 | 0.316 |

8. Stiffness tensor

Table S4 | Computed components of the stiffness tensor Cij (GPa) for all halide perovskites.

|  | C11 | C22 | C33 | C44 | C55 | C66 | C12 | C13 | C23 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| KPbI3 | 35 | 27 | 17 | 5 | 12 | 8 | 10 | 15 | 10 |
| RbPbI3 | 33 | 28 | 15 | 5 | 11 | 8 | 10 | 16 | 9 |
| CsPbI3 | 31 | 34 | 17 | 6 | 11 | 7 | 9 | 17 | 9 |
| FrPbI3 | 28 | 36 | 16 | 6 | 12 | 7 | 9 | 16 | 11 |
| MAPbI3 | 25 | 41 | 31 | 6 | 10 | 5 | 8 | 16 | 13 |
| KPbBr3 | 41 | 28 | 20 | 5 | 12 | 8 | 13 | 18 | 11 |
| RbPbBr3 | 39 | 33 | 18 | 6 | 13 | 9 | 12 | 19 | 12 |
| CsPbBr3 | 33 | 40 | 21 | 7 | 14 | 8 | 12 | 20 | 13 |
| FrPbBr3 | 31 | 42 | 22 | 6 | 14 | 8 | 12 | 20 | 15 |
| MAPbBr3 | 29 | 48 | 35 | 7 | 14 | 6 | 11 | 20 | 16 |
| KPbCl3 | 48 | 32 | 23 | 6 | 13 | 9 | 15 | 22 | 13 |
| RbPbCl3 | 43 | 37 | 22 | 6 | 13 | 9 | 15 | 22 | 15 |
| CsPbCl3 | 35 | 46 | 24 | 7 | 16 | 8 | 15 | 23 | 17 |
| FrPbCl3 | 35 | 48 | 28 | 7 | 17 | 8 | 13 | 25 | 17 |
| MAPbCl3 | 34 | 53 | 40 | 7 | 13 | 7 | 14 | 20 | 20 |
| KSnI3 | 35 | 29 | 17 | 5 | 13 | 8 | 10 | 16 | 9 |
| RbSnI3 | 33 | 33 | 17 | 5 | 12 | 8 | 9 | 17 | 10 |
| CsSnI3 | 27 | 36 | 21 | 6 | 12 | 7 | 9 | 16 | 10 |
| FrSnI3 | 26 | 36 | 21 | 6 | 14 | 7 | 9 | 18 | 12 |
| MASnI3 | 24 | 42 | 33 | 7 | 11 | 6 | 7 | 15 | 13 |
| KSnBr3 | 41 | 32 | 20 | 5 | 14 | 9 | 13 | 20 | 12 |
| RbSnBr3 | 38 | 38 | 20 | 6 | 13 | 9 | 12 | 20 | 13 |
| CsSnBr3 | 32 | 43 | 23 | 7 | 15 | 7 | 12 | 21 | 14 |
| FrSnBr3 | 34 | 46 | 31 | 7 | 19 | 7 | 10 | 23 | 13 |
| MASnBr3 | 33 | 48 | 38 | 7 | 13 | 7 | 12 | 19 | 16 |
| KSnCl3 | 48 | 36 | 26 | 6 | 15 | 10 | 16 | 24 | 15 |
| RbSnCl3 | 43 | 43 | 23 | 7 | 15 | 9 | 15 | 25 | 16 |
| CsSnCl3 | 35 | 49 | 31 | 8 | 17 | 8 | 14 | 25 | 18 |
| FrSnCl3 | 39 | 52 | 41 | 8 | 22 | 7 | 11 | 27 | 14 |
| MASnCl3 | 42 | 54 | 43 | 9 | 16 | 9 | 16 | 23 | 17 |

9. Compliance tensor

Table S5 | Computed components of the compliance tensor Sij (GPa-1) for all halide perovskites.

|  | S11 | S22 | S33 | S44 | S55 | S66 | S12 | S13 | S23 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| KPbI3 | 0.05 | 0.05 | 0.11 | 0.20 | 0.08 | 0.13 | 0.00 | -0.04 | -0.03 |
| RbPbI3 | 0.06 | 0.04 | 0.15 | 0.20 | 0.09 | 0.13 | 0.00 | -0.07 | -0.03 |
| CsPbI3 | 0.07 | 0.03 | 0.14 | 0.17 | 0.09 | 0.14 | 0.00 | -0.07 | -0.02 |
| FrPbI3 | 0.08 | 0.04 | 0.17 | 0.17 | 0.08 | 0.14 | 0.01 | -0.09 | -0.03 |
| MAPbI3 | 0.06 | 0.03 | 0.05 | 0.17 | 0.10 | 0.20 | 0.00 | -0.03 | -0.01 |
| KPbBr3 | 0.04 | 0.05 | 0.09 | 0.20 | 0.08 | 0.13 | -0.01 | -0.03 | -0.02 |
| RbPbBr3 | 0.05 | 0.04 | 0.13 | 0.17 | 0.08 | 0.11 | 0.00 | -0.06 | -0.03 |
| CsPbBr3 | 0.07 | 0.03 | 0.13 | 0.14 | 0.07 | 0.13 | 0.00 | -0.07 | -0.02 |
| FrPbBr3 | 0.08 | 0.03 | 0.13 | 0.17 | 0.07 | 0.13 | 0.00 | -0.07 | -0.03 |
| MAPbBr3 | 0.06 | 0.02 | 0.05 | 0.14 | 0.07 | 0.17 | 0.00 | -0.03 | -0.01 |
| KPbCl3 | 0.04 | 0.04 | 0.09 | 0.17 | 0.08 | 0.11 | 0.00 | -0.03 | -0.02 |
| RbPbCl3 | 0.05 | 0.04 | 0.11 | 0.17 | 0.08 | 0.11 | 0.00 | -0.05 | -0.03 |
| CsPbCl3 | 0.08 | 0.03 | 0.13 | 0.14 | 0.06 | 0.13 | 0.00 | -0.08 | -0.02 |
| FrPbCl3 | 0.08 | 0.03 | 0.11 | 0.14 | 0.06 | 0.13 | 0.00 | -0.07 | -0.02 |
| MAPbCl3 | 0.04 | 0.02 | 0.04 | 0.14 | 0.08 | 0.14 | 0.00 | -0.02 | -0.01 |
| KSnI3 | 0.05 | 0.04 | 0.11 | 0.20 | 0.08 | 0.13 | 0.00 | -0.05 | -0.02 |
| RbSnI3 | 0.06 | 0.04 | 0.14 | 0.20 | 0.08 | 0.13 | 0.00 | -0.06 | -0.02 |
| CsSnI3 | 0.07 | 0.03 | 0.09 | 0.17 | 0.08 | 0.14 | 0.00 | -0.05 | -0.01 |
| FrSnI3 | 0.10 | 0.03 | 0.13 | 0.17 | 0.07 | 0.14 | 0.00 | -0.08 | -0.02 |
| MASnI3 | 0.06 | 0.03 | 0.05 | 0.14 | 0.09 | 0.17 | 0.00 | -0.03 | -0.01 |
| KSnBr3 | 0.05 | 0.04 | 0.11 | 0.20 | 0.07 | 0.11 | 0.00 | -0.05 | -0.02 |
| RbSnBr3 | 0.06 | 0.03 | 0.12 | 0.17 | 0.08 | 0.11 | 0.00 | -0.06 | -0.02 |
| CsSnBr3 | 0.08 | 0.03 | 0.12 | 0.14 | 0.07 | 0.14 | 0.00 | -0.07 | -0.02 |
| FrSnBr3 | 0.06 | 0.02 | 0.07 | 0.14 | 0.05 | 0.14 | 0.00 | -0.04 | -0.01 |
| MASnBr3 | 0.04 | 0.02 | 0.04 | 0.14 | 0.08 | 0.14 | 0.00 | -0.02 | -0.01 |
| KSnCl3 | 0.04 | 0.04 | 0.08 | 0.17 | 0.07 | 0.10 | 0.00 | -0.03 | -0.02 |
| RbSnCl3 | 0.06 | 0.03 | 0.14 | 0.14 | 0.07 | 0.11 | 0.00 | -0.07 | -0.03 |
| CsSnCl3 | 0.07 | 0.03 | 0.09 | 0.13 | 0.06 | 0.13 | 0.00 | -0.05 | -0.02 |
| FrSnCl3 | 0.05 | 0.02 | 0.05 | 0.13 | 0.05 | 0.14 | 0.00 | -0.03 | -0.01 |
| MASnCl3 | 0.03 | 0.02 | 0.03 | 0.11 | 0.06 | 0.11 | -0.01 | -0.02 | -0.01 |

10. Bulk modulus B

Figure S5 | The polycrystalline bulk modulus B versus θw for (a) o-APbI3, (b) o-APbBr3, (c) o-APbCl3, (d) o-ASnI3, (e) o-ASnBr3, and (f) o-ASnCl3. Blue and orange symbols correspond to o-ABX3 inorganic and o-MABX3 hybrid halide perovskites respectively.

11. Shear modulus G

Figure S6 | The polycrystalline shear modulus G versus θw for (a) o-APbI3, (b) o-APbBr3, (c) o-APbCl3, (d) o-ASnI3, (e) o-ASnBr3, and (f) o-ASnCl3. Blue and orange symbols correspond to the o-ABX3 inorganic and o-MABX3 hybrid halide perovskites respectively.

12. Orientation of the hydrogen atoms along the b- and c-axes in o-MAPbI3

Figure S7 | (a) ac plane of o-MAPbI3 showing two H atoms on a MA cation oriented along the c-axis. (b) ab plane showing the other four H atoms on the MA cation oriented towards the b-axis. Dotted lines indicate hydrogen-bonding interactions between H and I atoms.

13. Deformation potentials

Figure S8 | Average deformation potential along the three crystal axes versus θw for (a) o-APbI3, (b) o-APbBr3, (c) o-APbCl3, (d) o-ASnI3, (e) o-ASnBr3, and (f) o-ASnCl3. Blue and orange symbols correspond to the o-ABX3 inorganic and o-MABX3 hybrid series respectively. Arrows represent variations of electron (e) and hole (h) deformation potentials caused by hydrogen-bonding induced octahedral tilting.

Notes on deformation potential calculation

We found that the deformation potential is very sensitive to the reference states chosen for the alignment of the eigenvalues during fitting. Many references were tested for band alignment including the Cl/Br/I 1s, Pb/Sn 1s and C/N/H/K/Rb/Cs/Fr 1s states but we found that the Cl/Br/I 1s core state produces the best reasonable value for linear least square fitting.

Table S6 | Computed electron (e) and hole (h) deformation potentials D (eV) along the a [100], b [010], and c [001] axes for all halide perovskites.

|  | Dh [100]a | De [100]a | Dh [010]b | De [010]b | Dh [001]c | De [001]c |
| --- | --- | --- | --- | --- | --- | --- |
| KPbI3 | -4.16 | -3.61 | -3.65 | -2.12 | -3.80 | -1.39 |
| RbPbI3 | -4.08 | -3.25 | -3.84 | -2.08 | -3.53 | -1.49 |
| CsPbI3 | -4.00 | -2.62 | -4.11 | -2.08 | -3.33 | -1.68 |
| FrPbI3 | -4.03 | -2.30 | -4.15 | -2.08 | -3.46 | -1.77 |
| MAPbI3 | -4.11 | -1.98 | -3.27 | -2.14 | -3.90 | -2.04 |
| KPbBr3 | -5.17 | -4.16 | -4.70 | -2.87 | -4.98 | -2.18 |
| RbPbBr3 | -5.27 | -3.81 | -5.26 | -2.77 | -4.71 | -2.15 |
| CsPbBr3 | -5.49 | -3.19 | -5.69 | -2.68 | -4.84 | -2.27 |
| FrPbBr3 | -5.55 | -2.89 | -5.69 | -2.69 | -5.01 | -2.29 |
| MAPbBr3 | -5.76 | -2.91 | -4.65 | -2.69 | -4.91 | -2.41 |
| KPbCl3 | -5.86 | -4.79 | -5.58 | -3.60 | -5.68 | -2.90 |
| RbPbCl3 | -6.08 | -4.47 | -6.08 | -3.44 | -5.61 | -2.87 |
| CsPbCl3 | -6.33 | -3.82 | -6.60 | -3.35 | -5.77 | -2.88 |
| FrPbCl3 | -6.40 | -3.32 | -6.75 | -3.41 | -6.31 | -3.05 |
| MAPbCl3 | -6.71 | -3.83 | -5.48 | -3.30 | -5.51 | -2.93 |
| KSnI3 | -5.58 | -4.74 | -5.09 | -1.48 | -5.00 | -0.77 |
| RbSnI3 | -5.57 | -4.03 | -5.47 | -1.75 | -4.86 | -0.97 |
| CsSnI3 | -5.72 | -2.60 | -5.85 | -2.59 | -5.18 | -1.41 |
| FrSnI3 | -6.01 | -2.40 | -6.21 | -3.09 | -5.86 | -2.01 |
| MASnI3 | -5.71 | -1.61 | -4.82 | -3.18 | -5.34 | -1.58 |
| KSnBr3 | -6.72 | -5.32 | -6.25 | -2.16 | -6.30 | -1.49 |
| RbSnBr3 | -6.90 | -4.57 | -6.93 | -2.41 | -6.22 | -1.66 |
| CsSnBr3 | -7.18 | -3.17 | -7.39 | -3.09 | -6.65 | -2.03 |
| FrSnBr3 | -7.36 | -2.59 | -7.78 | -3.24 | -7.48 | -2.53 |
| MASnBr3 | -7.55 | -2.94 | -6.45 | -3.24 | -6.36 | -2.05 |
| KSnCl3 | -7.47 | -5.97 | -7.06 | -2.86 | -7.13 | -2.23 |
| RbSnCl3 | -7.70 | -5.23 | -7.79 | -3.03 | -7.05 | -2.33 |
| CsSnCl3 | -8.06 | -3.47 | -8.44 | -3.75 | -7.92 | -2.90 |
| FrSnCl3 | -8.31 | -3.06 | -8.79 | -3.69 | -8.51 | -3.22 |
| MASnCl3 | -8.81 | -4.17 | -7.45 | -3.47 | -6.83 | -2.37 |

14. Effective charge carrier masses

Figure S9 | Average effective carrier mass along the three crystal axes versus θw for (a) o-APbI3, (b) o-APbBr3, (c) o-APbCl3, (d) o-ASnI3, (e) o-ASnBr3, and (f) o-ASnCl3. Blue and orange symbols correspond to the o-ABX3 inorganic and o-MABX3 hybrid series respectively. Arrows represent increases of electron (e) and hole (h) effective masses caused by hydrogen-bonding induced octahedral tilting.

Table S7 | Computed electron (e) and hole (h) effective carrier masses m* (in units of rest mass m0) along the a [100], b [010], and c [001] axes for all halide perovskites.

|  | m*h [100]a | m*e [100]a | m*h [010]b | m*e [010]b | m*h [001]c | m*e [001]c |
| --- | --- | --- | --- | --- | --- | --- |
| KPbI3 | 0.41 | 0.30 | 0.35 | 0.37 | 0.32 | 0.34 |
| RbPbI3 | 0.42 | 0.27 | 0.28 | 0.27 | 0.32 | 0.31 |
| CsPbI3 | 0.40 | 0.24 | 0.20 | 0.16 | 0.28 | 0.26 |
| FrPbI3 | 0.30 | 0.20 | 0.17 | 0.14 | 0.23 | 0.21 |
| MAPbI3 | 0.25 | 0.20 | 0.22 | 0.15 | 0.25 | 0.22 |
| KPbBr3 | 0.41 | 0.36 | 0.40 | 0.51 | 0.36 | 0.41 |
| RbPbBr3 | 0.37 | 0.33 | 0.29 | 0.31 | 0.34 | 0.36 |
| CsPbBr3 | 0.27 | 0.25 | 0.20 | 0.20 | 0.27 | 0.27 |
| FrPbBr3 | 0.23 | 0.22 | 0.18 | 0.17 | 0.23 | 0.23 |
| MAPbBr3 | 0.24 | 0.23 | 0.23 | 0.19 | 0.26 | 0.26 |
| KPbCl3 | 0.46 | 0.46 | 0.46 | 0.62 | 0.43 | 0.53 |
| RbPbCl3 | 0.39 | 0.39 | 0.34 | 0.41 | 0.38 | 0.44 |
| CsPbCl3 | 0.30 | 0.32 | 0.25 | 0.26 | 0.31 | 0.34 |
| FrPbCl3 | 0.25 | 0.27 | 0.22 | 0.23 | 0.25 | 0.27 |
| MAPbCl3 | 0.28 | 0.31 | 0.29 | 0.28 | 0.32 | 0.35 |
| KSnI3 | 0.25 | 0.30 | 0.20 | 0.43 | 0.20 | 0.22 |
| RbSnI3 | 0.21 | 0.26 | 0.15 | 0.25 | 0.17 | 0.20 |
| CsSnI3 | 0.12 | 0.18 | 0.08 | 0.11 | 0.11 | 0.16 |
| FrSnI3 | 0.09 | 0.14 | 0.06 | 0.08 | 0.08 | 0.13 |
| MASnI3 | 0.12 | 0.20 | 0.10 | 0.09 | 0.13 | 0.21 |
| KSnBr3 | 0.26 | 0.34 | 0.25 | 0.63 | 0.23 | 0.26 |
| RbSnBr3 | 0.21 | 0.30 | 0.16 | 0.31 | 0.19 | 0.23 |
| CsSnBr3 | 0.13 | 0.22 | 0.10 | 0.14 | 0.13 | 0.19 |
| FrSnBr3 | 0.09 | 0.14 | 0.07 | 0.10 | 0.08 | 0.14 |
| MASnBr3 | 0.13 | 0.22 | 0.11 | 0.15 | 0.14 | 0.21 |
| KSnCl3 | 0.31 | 0.42 | 0.32 | 0.82 | 0.29 | 0.34 |
| RbSnCl3 | 0.25 | 0.37 | 0.21 | 0.41 | 0.25 | 0.31 |
| CsSnCl3 | 0.16 | 0.26 | 0.13 | 0.19 | 0.15 | 0.25 |
| FrSnCl3 | 0.11 | 0.19 | 0.10 | 0.16 | 0.11 | 0.19 |
| MASnCl3 | 0.15 | 0.27 | 0.16 | 0.24 | 0.18 | 0.25 |

15. Charge carrier mobility

Table S8 | Computed electron (e) and hole (h) mobilities  (cm2/V·s) at 100 K along the a [100], b [010], and c [001] axes for all halide perovskites.

|  | h [100]a | e [100]a | h [010]b | e [010]b | h [001]c | e [001]c |
| --- | --- | --- | --- | --- | --- | --- |
| KPbI3 | 5930 | 17165 | 8733 | 22448 | 6609 | 42306 |
| RbPbI3 | 5546 | 26323 | 14609 | 54387 | 6664 | 40847 |
| CsPbI3 | 5981 | 50044 | 35703 | 242819 | 11641 | 55487 |
| FrPbI3 | 11141 | 93714 | 55729 | 360166 | 16804 | 80425 |
| MAPbI3 | 15097 | 114133 | 53960 | 327720 | 20880 | 105133 |
| KPbBr3 | 4491 | 9626 | 4044 | 5896 | 3221 | 12166 |
| RbPbBr3 | 5317 | 13553 | 8294 | 25353 | 3790 | 15839 |
| CsPbBr3 | 9322 | 33522 | 22139 | 99755 | 7489 | 34142 |
| FrPbBr3 | 12553 | 51667 | 30289 | 156021 | 10889 | 52270 |
| MAPbBr3 | 9802 | 42855 | 27554 | 132713 | 13505 | 55900 |
| KPbCl3 | 3072 | 4588 | 2272 | 2585 | 1865 | 4239 |
| RbPbCl3 | 3907 | 7245 | 4758 | 9338 | 2500 | 6640 |
| CsPbCl3 | 5643 | 13162 | 10640 | 37502 | 4316 | 13775 |
| FrPbCl3 | 8659 | 26517 | 14712 | 51644 | 7177 | 25367 |
| MAPbCl3 | 5747 | 13663 | 12382 | 37226 | 7178 | 20284 |
| KSnI3 | 11285 | 9899 | 20020 | 34988 | 12309 | 411248 |
| RbSnI3 | 16686 | 18641 | 39857 | 108325 | 19624 | 326311 |
| CsSnI3 | 52805 | 92935 | 185905 | 427905 | 60411 | 321156 |
| FrSnI3 | 94117 | 195595 | 334177 | 657575 | 108550 | 273596 |
| MASnI3 | 47349 | 167268 | 180799 | 540424 | 60092 | 206966 |
| KSnBr3 | 8308 | 6786 | 8340 | 6943 | 6441 | 84314 |
| RbSnBr3 | 12523 | 11714 | 24518 | 38759 | 10480 | 91602 |
| CsSnBr3 | 31990 | 44112 | 79639 | 196194 | 26678 | 110970 |
| FrSnBr3 | 81224 | 216451 | 187772 | 443736 | 98322 | 212853 |
| MASnBr3 | 29772 | 52624 | 91449 | 166398 | 40792 | 143043 |
| KSnCl3 | 5062 | 3712 | 3912 | 2264 | 3532 | 24285 |
| RbSnCl3 | 7389 | 6012 | 11127 | 13783 | 4784 | 25651 |
| CsSnCl3 | 16700 | 26746 | 36054 | 70623 | 18021 | 37377 |
| FrSnCl3 | 45119 | 84782 | 67936 | 119297 | 44671 | 79477 |
| MASnCl3 | 19877 | 20437 | 30360 | 50788 | 21167 | 77164 |

Table S9 | Computed electron (e) and hole (h) mobilities  (cm2/V·s) at 300 K along the a [100], b [010], and c [001] axes for all halide perovskites.

|  | h [100]a | e [100]a | h [010]b | e [010]b | h [001]c | e [001]c |
| --- | --- | --- | --- | --- | --- | --- |
| KPbI3 | 1137 | 3301 | 1689 | 4429 | 1242 | 7994 |
| RbPbI3 | 1077 | 4903 | 2692 | 10464 | 1293 | 8108 |
| CsPbI3 | 1157 | 9758 | 7157 | 44701 | 2271 | 10951 |
| FrPbI3 | 2181 | 17536 | 10607 | 74258 | 3116 | 15131 |
| MAPbI3 | 2986 | 21668 | 10747 | 64657 | 3825 | 21029 |
| KPbBr3 | 862 | 1821 | 762 | 1127 | 637 | 2412 |
| RbPbBr3 | 1015 | 2708 | 1625 | 4721 | 726 | 2992 |
| CsPbBr3 | 1737 | 6255 | 4187 | 19861 | 1504 | 6528 |
| FrPbBr3 | 2309 | 9528 | 5645 | 29195 | 2064 | 9602 |
| MAPbBr3 | 1925 | 8076 | 5237 | 24025 | 2684 | 10643 |
| KPbCl3 | 576 | 871 | 445 | 501 | 365 | 834 |
| RbPbCl3 | 748 | 1372 | 892 | 1769 | 468 | 1313 |
| CsPbCl3 | 1061 | 2587 | 2140 | 6995 | 838 | 2705 |
| FrPbCl3 | 1638 | 5137 | 2830 | 9763 | 1409 | 4801 |
| MAPbCl3 | 1082 | 2695 | 2388 | 7477 | 1345 | 3790 |
| KSnI3 | 2278 | 1973 | 3677 | 6664 | 2343 | 78177 |
| RbSnI3 | 3264 | 3657 | 8251 | 20108 | 3592 | 66035 |
| CsSnI3 | 9313 | 16868 | 33249 | 88977 | 11546 | 66044 |
| FrSnI3 | 20031 | 40155 | 61048 | 134985 | 19829 | 53838 |
| MASnI3 | 8231 | 33449 | 38204 | 95096 | 12068 | 39757 |
| KSnBr3 | 1541 | 1282 | 1607 | 1337 | 1213 | 16006 |
| RbSnBr3 | 2446 | 2280 | 4497 | 7331 | 1975 | 17409 |
| CsSnBr3 | 6001 | 8585 | 15720 | 36005 | 5589 | 21583 |
| FrSnBr3 | 17531 | 39083 | 35911 | 75835 | 17174 | 41338 |
| MASnBr3 | 6306 | 10700 | 15776 | 33699 | 8352 | 27283 |
| KSnCl3 | 951 | 726 | 780 | 434 | 667 | 4530 |
| RbSnCl3 | 1412 | 1146 | 2102 | 2587 | 963 | 4972 |
| CsSnCl3 | 3460 | 5028 | 6956 | 12886 | 3363 | 7539 |
| FrSnCl3 | 8238 | 17285 | 12194 | 21463 | 8502 | 15883 |
| MASnCl3 | 3703 | 3875 | 5853 | 9584 | 4125 | 14372 |

Figure S10 | Average electron (e) and hole (h) mobilities along the three crystal axes versus θw for (a) o-APbI3, (b) o-APbBr3, (c) o-APbCl3, (d) o-ASnI3, (e) o-ASnBr3, and (f) o-ASnCl3. Blue and orange symbols correspond to o-ABX3 inorganic and o-MABX3 hybrid halide perovskites, respectively. Arrows indicate the reduction in the e and h mobilities of o-MABX3 with respect to what they would have been for hypothetical o-ABX3 perovskites having the same size A-site cation. The arrows follow the extrapolated trend lines. The values are calculated at 300 K.

References

(1) 	Perdew, J. P.; Ruzsinszky, A.; Csonka, G. I.; Vydrov, O. A.; Scuseria, G. E.; Constantin, L. A.; Zhou, X.; Burke, K. Phys. Rev. Lett. 2008, 100, 136406.

(2) 	Klimeš, J.; Bowler, D. R.; Michaelides, A. J. Phys. Condens. Matter 2010, 22, 022201.

(3) 	Klimeš, J.; Bowler, D. R.; Michaelides, A. Phys. Rev. B 2011, 83, 195131.

(4) 	Lee, K.; Murray, É. D.; Kong, L.; Lundqvist, B. I.; Langreth, D. C. Phys. Rev. B 2010, 82, 081101.

(5) 	Tkatchenko, A.; Scheffler, M. Phys. Rev. Lett. 2009, 102, 6.

(6) 	Sun, J.; Ruzsinszky, A.; Perdew, J. P. Phys. Rev. Lett. 2015, 115, 036402.

(7) 	Weller, M. T.; Weber, O. J.; Henry, P. F.; Di Pumpo, A. M.; Hansen, T. C. Chem. Commun. 2015, 51, 4180.

(8) 	Shannon, R. D. Acta Cryst. 1976, A32, 751.