# The Ceramic Building Materials
## Dr Philip Mills MIfA (Updated December 2013)
## Introduction
Some 2034 fragments, weighing 89.056 kg of Ceramic Building Materials (CBM) were submitted for analysis. Around1130 fragments were recovered from stratified contexts (67kg).
The material was studied in July and November 2007, with the final analysis report update in May 2009 following the availability of the final phasing. The full assemblage was coded onto an Access 2000 database, with fragments grouped by context and ‘sherd families’ defined by fabric, form and depositional traces (such as sooting and mortar). Each group was quantified by fragment count (No), weight in grams (Wt), corner count (Cnr), with derived minimum numbers being given by ‘ Tile equivalents’ (taking each corner as representing 25% of a complete tile) and minimum number of tiles by context (‘MT’) where an estimate was made taking into account which corners were present. Other characteristics such as the presence of marks, tallies or sooting were also noted. The mean sherd weight (MSW) is derived by dividing the total weight of a family of sherds by the total number.
## Chronology
The main fabrics identified in the assemblage were not in themselves indicative of date, although the main forms of tegula and imbrex were definitely Roman date; a more precise date is suggested by the identification of two types of lower cutaway (Warry 2006, types 15 and 16, Class D) which suggest a date of AD240 – 380.
Table 1 The CBM assemblage by phase group
Phase	No%	Wt%	Cnr%	MT%	TE%	MSW
1b	0.1%	0.0%		0.0%	0.0%	4.00
3a	2.4%	2.0%	3.9%	5.4%	4.9%	50.59
3b	1.0%	0.1%		0.0%	0.0%	6.64
3c	10.9%	4.6%	3.9%	5.4%	4.9%	24.90
3d	16.8%	5.4%	3.9%	5.4%	4.9%	19.18
4a	38.3%	64.8%	70.1%	62.2%	62.3%	100.17
5a	30.1%	23.0%	18.2%	21.6%	22.95%	44.66
N	1136	67267	77	37	1525	59.21

Table 1 shows the breakdown of the stratified assemblage by phase. There is a small quantity of intrusive material in phases 1 and 2, with the first substantial quantities appearing in phase 3. The CBM entering the archaeological record at this stage would have been from breakages during construction (Presumably Phase 3A) and slightly larger quantities during refurbishment remodelling events later in the life cycle of the site. The majority of the Tile is from phase 4, which is consistent with deposits of collapsed roof which is largely undisturbed except by wall robbing and ploughing.
## Taphonomy
The context descriptions have been sorted by standard context type definitions, (following Booth 2000, Mills 2006), which allows some comparison with CBM assemblages from other sites. Table 2 gives the breakdown of the entire assemblage by context type, as well as the changing MSW by context type. This is illustrated in Figures 1 and 2. The largest quantity of material is from collapse deposits, consistent with the pattern suggested from the phase group data. On most sites Ditch and Pit deposits are much more common as a final discarding point of CBM fragments regarded as refuse. This pattern to some degree is seen here, albeit with a much small proportion of the assemblage coming from these deposits than normally. The small fragment size is indicated by higher No% figures to Wt% values as well as the MSW figures. There is a high level of material from construction deposits, reflecting the rural nature of the site so CBM is only really brought in for the initial construction. There is a small spike of material from hearth deposits, reflecting some complete in situ pieces from such deposits. The complete examples from hearths are the cause of the large spike in the MSW value. The other three sources of large fragments of CBM are the collapse deposits, underlining the relatively undisturbed nature of these deposits on this site, construction layers where large fragments would have been selected for this use and the somewhat smaller reworked fragments from robber deposits.
The breakdown of CBM by context type by deposit type by phase group is illustrated as a proportional stacked bar chart in Figure 3 and the MSW values by phase site are shown as a stacked bar chart in figure 4. Ignoring the intrusive material from the IA phases we see the expected importance of construction and floor layers in phase 3a and 3b (whose small size makes meaningful analysis difficult). There is an interesting suggestion of the rise of dumping of CBM in the ditch fills in phase 3C, along side some restructuring (as ‘robbing’ activity). It is perhaps of note that in phase 3c deposition of refuse CBM occurs in the Midden deposits rather than the ditch. As expected the latter phases are dominated by collapse and then robbing, although the CBM refuse in pits in phase 5 is of note, with fragments which are smaller than collapse of robbing deposit fragments.
Table 2 CBM by context type
Cxt Class	No%	Wt%	Cnr%	MT%	TE%	MSW
Collapse	47.1%	70.1%	72.7%	67.6%	65.6%	88.18
Construction layer	2.8%	3.2%	5.2%	8.1%	6.6%	68.31
Ditch	8.7%	1.8%	2.6%	2.7%	3.3%	12.42
Floor layer	0.7%	0.2%		0.0%	0.0%	16.13
Hearth/oven	0.4%	1.9%	3.9%	5.4%	4.9%	252.60
Layer	1.2%	0.4%		0.0%	0.0%	18.64
Midden	0.4%	0.2%		0.0%	0.0%	25.25
Pit	2.6%	1.1%		0.0%	0.0%	24.83
Pond	0.1%	0.0%		0.0%	0.0%	7.00
Posthole	0.2%	0.0%		0.0%	0.0%	3.50
Robber Trench	35.7%	21.1%	15.6%	16.2%	19.7%	34.89
N	1136	67267	77	37	1525	59.21

Figure 1 Bar chart of CBM quantities by context type

Figure 2 Bar chart of MSW by context type

Table 3 CBM by context type by phase
Phase	Cxt Class	No%	Wt%	Cnr%	MT%	TE%	MSW	N no	N wt	N Cnr	N MT	N TE
1b	Pit	100.00%	100.00%				4	1	4		0	0
3a	Construction layer	62.96%	91.43%	100.00%	100.00%	100.00%	73.470588	27	1366	3	2	75
3a	Floor layer	3.70%	0.95%		0.00%	0.00%	13	27	1366	3	2	75
3a	Layer	33.33%	7.61%		0.00%	0.00%	11.555556	27	1366	3	2	75
3b	Collapse	36.36%	8.22%				1.5	11	73		0	0
3b	Construction layer	9.09%	20.55%				15	11	73		0	0
3b	Ditch	9.09%	5.48%				4	11	73		0	0
3b	Floor layer	45.45%	65.75%				9.6	11	73		0	0
3c	collapse	10.48%	36.04%		0.00%	0.00%	85.615385	124	3088	3	2	75
3c	Construction layer	3.23%	18.26%	33.33%	50.00%	33.33%	141	124	3088	3	2	75
3c	Ditch	79.03%	39.70%	66.67%	50.00%	66.67%	12.510204	124	3088	3	2	75
3c	Layer	4.03%	5.08%		0.00%	0.00%	31.4	124	3088	3	2	75
3c	Pit	0.81%	0.45%		0.00%	0.00%	14	124	3088	3	2	75
3c	Pond	0.81%	0.23%		0.00%	0.00%	7	124	3088	3	2	75
3c	Posthole	1.61%	0.23%		0.00%	0.00%	3.5	124	3088	3	2	75
3d	Floor layer	1.05%	1.86%		0.00%	0.00%	34	191	3664	3	2	75
3d	Hearth/oven	2.62%	34.47%	100.00%	100.00%	100.00%	252.6	191	3664	3	2	75
3d	Midden	2.09%	2.76%		0.00%	0.00%	25.25	191	3664	3	2	75
3d	Robber Trench	94.24%	60.92%		0.00%	0.00%	12.4	191	3664	3	2	75
4a	collapse	100.00%	100.00%	100.00%	100.00%	100.00%	94.772443	479	45396	56	25	1000
5a	Collapse	23.9%	16.0%	14.3%	25.0%	14.3%	29.86
5a	Construction layer	2.9%	2.3%				35.8
5a	Pit	9.24%	5.32%				26.0
5a	Robber Trench	65.1%	77.0%	85.7%	75.0%	85.7%	52.8	347	15496	14	8	350

Figure 3 Proportional stacked bar chart of CBM by No% by context type by phase

Figure 4 Stacked bar chart of MSW by context type
## Supply
The different quantities of the fabrics identified are shown in Table 4. The majority of roof tile are from closely related fabrics T03. T03.1 and t03.2.Thee is a small quantity of T26 which may be some second hand building material brought in for the refurbishments in phase 3d.
Table 4 Fabric proportions
Fabric	No%	Wt%	Cnr%	MT%	TE%	MSW
T03	79.0%	76.6%	59.7%	59.5%	67.2%	57.41
T03.1	13.8%	20.5%	37.7%	37.8%	29.5%	87.71
T03.2	6.6%	1.4%		0.0%	0.0%	12.41
T26	0.4%	1.5%	2.6%	2.7%	3.3%	249.25
N	1136	67267	77	37	1525	59.21391

Figure 5 Bar chart of quantities of different fabrics
## Class T, Roman roof tile
### T03 (79%) Crambeck Oxidised roof tile
A hard fabric with an irregular fracture and sandy feel, it is reddish yellow (5YR6/6) with inclusions of moderate quartz and red iron stone with some finer black iron stone.
This is the most abundant fabric in all phases, although there is something of a decline in phase 3c and 4a.The forms in this fabric were all tegula and imbrex, although the only cutaway forms present were of the later date, suggesting the whole sale removal of many of the earlier tiles in this fabric

Table 5 Form catalogue for T023
Form Code	Description
I1.1	A curved wall Imbrex with straight edges.
TE1.1	This is a tegula with flanges which are straight with a concave indentation on the internal face.
TE1.2	This is a tegula with a straight flange with an inward sloping top and a straight or slightly inwardly bowing inner face. It has lower cutaway of Warry (2006) type 16. AD260-380
TE1.2a	This is a tegula with a straight flange with an inward sloping top and a straight or slightly inwardly bowing inner face. It has lower cutaway of Warry (2006) type 15. AD260-380
Te1.3	This is a tegula with a flange with a straight outer face, hand moulded top and straight inner face and groove at foot of inner face. It has lower cutaway of Warry (2006) type 16. AD260-380
TE1.4	This is a tegula with a flat squared flange, having a slightly concave top and small ridge at base of the inner face. It has lower cutaway of Warry (2006) type 16. AD260-380

### T03.1 (14%)
This is a hard fabric with an irregular fracture and harsh feel. It has red (2.5YR 5/6) margins and surfaces with a grey core. It has inclusions of occasional quartz at 0, 5 mm and rounded black iron stone at 0.3 mm in a common sandy matrix. High fired.
In addition to the same range of tegula and imbrex forms in fabric T03, also noticeable for the absence of early cutaways, is the presence of a few fragments of concave tegula. Warry suggests that these are used for partial dome structures in Romano-British structures. The absence of any evidence for a bath house here would suggest that concave tegula were used in the original structure to highlight a specific attribute of the building – most likely the original doorway/ entrance vestibule. The location of the different concave tegula fragments is given in Table 6.
Table 6 Form catalogue for T03.1
Form Code	Description
I1.1	A curved wall Imbrex with straight edges.
TE1.1	This is a tegula with flanges which are straight with a concave indentation on the internal face. It has lower cutaway of Warry (2006) type 15 AD260-380.
TE1.2	This is a tegula with a straight flange with an inward sloping top and a straight or slightly inwardly bowing inner face. It has lower cutaway of Warry (2006) type 16 AD260-380.
TE1.2a	This is a tegula with a straight flange with an inward sloping top and a straight or slightly inwardly bowing inner face. It has lower cutaway of Warry (2006) type 15. AD3260-380
TE2.0	This is a concave tegula (Warry 2006, 110)
TE2.1	This is a concave tegula (Warry 2006, 110) with smoothed underside and having flanges which are straight, with a flat top and a concave inner face.
TE2.5	This is a concave tegula (Warry 2006, 110) with a hand finished straight flange with top rising to outer face.

Table 7 Contexts from which concave tegula were recovered.
Phase	Context	Cxt Class	Code	No	Wt
3c	84	collapse	TE2.5	1	666
4a	50	Collapse	TE2.1	1	365
5a	41	Pit	TE2.5	1	392

### T03.2 (6%)
This is a hard fabric with a fine fracture and powdery feel. It is light red (10R 7/6) with inclusions of sparse lime in a sandy matrix.
This fabric is perhaps more like a pottery fabric rather than a tile fabric. All the examples of this fabric apparently come from the same roof finial. Table 8 shows all the locations where fragments of this item were recovered. The fragments from layers in phase 3a are almost certainly intrusive – the deposit types that these come from could well include later trample. It is most likely that this was roof furniture on the original structure which was removed during the refurbishments of phase 3c (or possibly damaged in a collapse event), and fragments thrown away as refuse.
#### Finnial
This is an example of roof furniture with arched cutaways, with pie crust decorated ridges. The contexts from which these fragments were recovered is given in Table 8
Table 8 Contexts from which finial fragments were recovered.
Phase	Cxt Class	Context
2b	Ditch	289
3a	Layer	19
3a	Layer	20
3c	collapse	84
3c	Ditch	109
3c	Ditch	167
3c	Ditch	167
3c	Ditch	91
3c	Ditch	91
3c	Ditch	98
4a	Collapse	56
5a	collapse	87
5a	Pit	41
5a	Robber Trench	51
5a	Robber Trench	70
5a	Robber Trench	96
6a	Topsoil/ Ploughsoil	37
6a	Topsoil/ Ploughsoil	37
6a	Topsoil/ Ploughsoil	82

### T26 (less than 1%)
This is a hard file fabric with a fine fracture and powdery feel. It has light red (2.5YR) margins and surfaces with a grey core. It has inclusions of common flint up to 1mm, occasional rounded quartz up to 0.5 mm, sparse clay pellets at 1mm sparse lime at 0.3mm and sparse fine silver mica.
All examples in this fabric come from a tegula from Hearth context (226). The fabric may be a tegula which has been specially bought in as use of a hearth liner, presumable at a point when roof tile for or from the rest of the structure was not available.
Table 9 Forms in T26
Form	Description
TE1.1	This is a tegula with flanges which are straight with a concave indentation on the internal face.

## Animal Prints
Overall there was a single incidence of human prints on a tile, on and example of TE3.1TE1.2 from (145) phase 3d making up 0.09% of the assemblage.
## Functional analysis
The grouping of the assemblage by main form type is shown in Table 10, with the breakdown by phase shown in Table 11. The changing composition in terms of form by phase group is illustrated as a proportional stacked bar chart in Fig 6. In the overall figures the ratio of imbrex to tegula is slightly higher than is usually the case for a relatively undisturbed roof collapse assemblage (Mills 2006). The breakdown by phase would suggest that this slight change is down to ploughed material from phase 5, where larger tegula pieces may well have been removed to facilitate the agricultural reuse of the land. This would more than offset the slight bias in favour of tegula ( compared to what would be expected for an assemblage of this nature) in phase 3a, where the material is likely to be stray breakages from the original construction, somewhat emphasised by the high proportion of imbrex by minimum count values.
Table 10 Form groups
Brick Type	No%	Wt%	Cnr%	MT%	TE%	MSW
B/T	37.1%	6.9%		0.0%	0.0%	10.9
Finial	6.8%	1.4%		0.0%	0.0%	12.2
Imbrex	12.7%	20.3%	41.6%	29.7%	31.1%	94.7
Tegula	43.4%	71.5%	58.4%	70.3%	68.9%	97.5
N	1136	67267	77	37	1525	59.2

Table 11 Form types by phase
Phase	Brick Type	No%	Wt%	Cnr%	MT%	TE%	N no	N wt	N Cnr	N MT	N TE
1b	B/T	100.0%	100.0%				1	4		0	0
3a	B/T	48.1%	5.5%		0.0%	0.0%
3a	finial	7.4%	3.1%		0.0%	0.0%
3a	Imbrex	7.4%	42.9%	66.7%	50.0%	66.7%
3a	Tegula	37.0%	48.5%	33.3%	50.0%	33.3%	27	###	3	2	75
3b	B/T	81.8%	74.0%
3b	finial	9.1%	5.5%
3b	Tegula	9.1%	20.5%				11	73		0	0
3c	B/T	35.5%	8.1%		0.0%	0.0%
3c	finial	45.2%	18.9%		0.0%	0.0%
3c	Imbrex	1.6%	2.7%		0.0%	0.0%
3c	Tegula	17.7%	70.3%	100.0%	100.0%	100.0%	124	###	3	2	75
3d	B/T	57.6%	13.5%		0.0%	0.0%
3d	Imbrex	3.1%	11.8%		0.0%	0.0%
3d	Tegula	39.3%	74.7%	100.0%	100.0%	100.0%	191	###	3	2	75
4a	B/T	24%	6%		0.0%	0.0%
4a	finial	0.%	0.0%		0.0%	0.0%
4a	Imbrex	13%	16%	41%	26.0%	26%
4a	Tegula	636%	78%	59%	74%	74%	435	43576	54	23	950
5a	B/T	441%	8%
5a	finial	5%	2%
5a	Imbrex	22%	36%	57%	50	50%
5a	Tegula	32%	54%	43%	50%	50%	347	15496	14	8	350

Figure 6 Proportional stacked bar chart of form by phase
## Burnt sherds
A summary of the burnt sherds is present in Table 12. The overall figure, at 2%, is very low for a rural figure and may be explained by the absence of any hypocaust tiles or any bath house type structure. The breakdown by phase is much the same, with the exception of phase 3a, the 7% value being the result of the relatively small sample size from that phase.
Table 12 Proportion of burnt CBM
Phase	N0%	Wt%	Cnr%	MT%	TE%	MSW	N no	N wt	N cnr	N mt	N te%
Overall	2%	5%	9%	14%	11%	140	1130	67223	77	37	1525
3a	7%	43%	67%	50%	67%	293	27	1366	3	2	75
3c	2%	20%	100%	100%	100%	207	123	3082	3	2	75
4a	3%	4%	9%	5%	5%	114	435	45576	54	23	950
5a	1%	1%	0%	0%	0%	80	347	15496	14	8	350

## Discussion

The structure was fully or partially roofed in tile manufactured at the Crambeck kilns. Only later tegula cutaways were recovered, and different cutaway types cannot be used in the same roof, it seems likely that this was the only roof during the lifetime of the building. The different fabric types may represent a continuum of products from the same source, or may be the result of patching. What evidence does survive suggest that there were two roof finials, which may have been broken in a third century collapse event, and an unusual concave feature, evidenced by the concave tegulae,, probably above or indicating an elaborate entrance vestibule
Most of the assemblage is from a later roof from the third/ fourth century refurbishment. The ratios of tegula to imbrex, and sherd size suggest that after the final collapse of the structure the roof tile was largely undisturbed, apart from where it would have to be moved to enable the remaining walls to be robbed, and later larger pieces would have been removed to facilitate the agricultural re working of the land. The small quantity of minimal numbers of tiles, based on surviving corners as well as the stone roofing tiles, suggests that the roof, at least, comprised an area partially tiled in red ceramic tiles enhanced by a roof structures made up grey stone slate. This makes some sense if ceramic roof tile is considered a high cost high status symbol, and in the long distance impact on a landscape of relatively small number could be enhanced with a striking contrast with the local stone tiles, which presumably would be more familiar in contemporary structures in the area.

# Bibliography
Booth, P Oxford Archaeology Roman Pottery Recording System: An Introduction Oxford Archaeology unpublished
Brodbribb G. 1989	Roman Brick and Tile Wolfboro: Alan Sutton.
Mills, P.J.E. 2006 The Ancient Mediterranean Trade in Ceramic Building Material: A Case Study in Carthage and Beirut. Unpublished PhD Thesis, University of Leicester, December 2005.
Warry 2006	Tegulae. Manufacture, typology and use in Roman Britain. Oxford: BAR British Series 417
## Appendix 1 Fabrics by phase

Fabric	Phase	No%	Wt%	Cnr%	MT%	TE%	MSW	N No	N Wt	N Cnr	N MT	N TE%
T03	1b	100.0%	100.0%				4.0	1	4		0	0
T03	3a	55.6%	31.3%		0.0%	0.0%	28.5	27	1366	3	2	75
T03	3b	81.8%	86.3%				7.0	11	73		0	0
T03	3c	23.4%	45.1%	100.0%	100.0%	100.0%	48.0	124	3088	3	2	75
T03	3d	96.9%	59.6%		0.0%	0.0%	11.8	191	3664	3	2	75
T03	4a	89.4%	86.3%	64.8%	65.2%	78.9%	96.7	435	43576	54	23	950
T03	5a	77.8%	63.8%	57.1%	62.5%	57.1%	36.6	347	15496	14	8	350
T03.1	3a	37.0%	65.6%	100.0%	100.0%	100.0%	89.6	27	1366	3	2	75
T03.1	3b	9.1%	8.2%				6.0	11	73		0	0
T03.1	3c	31.5%	36.0%		0.0%	0.0%	28.5	124	3088	3	2	75
T03.1	3d	1.0%	13.2%	33.3%	50.0%	33.3%	241.0	191	3664	3	2	75
T03.1	4a	10.1%	13.7%	35.2%	34.8%	21.1%	135.4	435	43576	54	23	950
T03.1	5a	17.6%	34.3%	42.9%	37.5%	42.9%	87.1	347	15496	14	8	350
T03.2	3a	7.4%	3.1%		0.0%	0.0%	21.5	27	1366	3	2	75
T03.2	3b	9.1%	5.5%				4.0	11	73		0	0
T03.2	3c	44.4%	18.7%		0.0%	0.0%	10.5	124	3088	3	2	75
T03.2	4a	0.2%	0.0%		0.0%	0.0%	6.0	435	43576	54	23	950
T03.2	5a	4.6%	1.9%		0.0%	0.0%	18.8	347	15496	14	8	350
t05.2	3c	0.8%	0.2%		0.0%	0.0%	6.0	124	3088	3	2	75
t05.2	4a	0.2%	0.0%		0.0%	0.0%	6.0	435	43576	54	23	950
t26	3d	2.1%	27.2%	66.7%	50.0%	66.7%	249.3	191	3664	3	2	75

## Appendix 2 Forms by Phase
Fabric	Form Code	Phase	No%	Wt%	Cnr%	MT%	TE%	MSW	N N0	N Wt	N Cnr	N MT	N TE%
T03	I1.1	3d	1.0%	2.6%		0.0%	0.0%	48	191	3664	3	2	75
T03	I1.1	4a	3.2%	9.3%	14.8%	8.7%	21.1%	289.14	435	43576	54	23	950
T03	I1.1	5a	0.6%	0.4%		0.0%	0.0%	29.5	347	15496	14	8	350
T03	TE00	4a	0.5%	0.9%	1.9%	4.3%	2.6%	200	435	43576	54	23	950
T03	TE1.1	4a	1.1%	1.3%		0.0%	0.0%	109.4	435	43576	54	23	950
T03	TE1.2	3d	1.0%	1.6%		0.0%	0.0%	29.5	191	3664	3	2	75
T03	TE1.2	4a	6.9%	26.8%	25.9%	26.1%	26.3%	389.83	435	43576	54	23	950
T03	TE1.2	5a	2.0%	11.0%	35.7%	25.0%	35.7%	242.71	347	15496	14	8	350
T03	TE1.2a	5a	0.3%	1.3%		12.5%	7.1%	201	347	15496	14	8	350
T03	TE1.3	4a	3.9%	16.5%	16.7%	21.7%	21.1%	423.35	435	43576	54	23	950
T03	Te1.3	5a	0.3%	1.6%		0.0%	0.0%	241	347	15496	14	8	350
T03	TE1.4	3c	0.8%	17.3%	33.3%	50.0%	33.3%	535	124	3088	3	2	75
T03	TE1.4	4a	0.7%	2.7%	5.6%	4.3%	7.9%	386	435	43576	54	23	950
T03	TE1.4	5a	0.3%	2.7%		0.0%	0.0%	415	347	15496	14	8	350
T03.1	I1.1	3d	0.5%	5.9%		0.0%	0.0%	216	191	3664	3	2	75
T03.1	I1.1	5a	0.3%	0.9%		0.0%	0.0%	141	347	15496	14	8	350
T03.1	TE00	3a	18.5%	21.1%	33.3%	50.0%	33.3%	57.6	27	1366	3	2	75
T03.1	Te00	3c	0.8%	1.7%		0.0%	0.0%	53	124	3088	3	2	75
T03.1	TE1.1	4a	0.7%	3.3%	1.9%	8.7%	5.3%	477	435	43576	54	23	950
T03.1	TE1.2	3d	0.5%	7.3%	33.3%	50.0%	33.3%	266	191	3664	3	2	75
T03.1	TE1.2	4a	0.9%	4.1%	7.4%	8.7%	10.5%	451.25	435	43576	54	23	950
T03.1	TE1.2a	5a	0.3%	4.3%	7.1%	12.5%	7.1%	670	347	15496	14	8	350
T03.1	TE2.1	4a	0.2%	0.8%		0.0%	0.0%	365	435	43576	54	23	950
T03.1	TE2.5	3c	0.8%	21.6%		0.0%	0.0%	666	124	3088	3	2	75
T03.1	Te2.5	5a	0.3%	2.5%		0.0%	0.0%	392	347	15496	14	8	350
t26	TE1.1	3d	2.1%	27.2%	66.7%	50.0%	66.7%	249.25	191	3664	3	2	75

Figure 7 T03 x10

Figure 8 T03.1 x10

Figure 9 T03.2 x10

Figure 10 T26 x10